## Slide 1
CHIP is a very generic term in the market, but these can be sub-divided into different Families
Integrated Circuits
MEMS
Silicon Photonics
(Microelectromechanical systems)
Types of Chips

## Slide 2: What are MEMS
Think of MEMS devices as the interface between the digital realm and the analogue world.
The digital IC comprises of ‘1’s and ‘0’s, whilst the MEMS devices are sensors and actuators.
Accelerometer
Gyroscope
Gears
(Micro/electro/mechanical/systems)

## Slide 3
Process Modules In the Fab
Photolithography
Etching
Chemical Vapor Deposition (CVD)
Physical Vapor Deposition (PVD)
Chemical Mechanical Polishing (CMP)
Diffusion
Implantation
Cleaning
Yield Defect Density (YDD)
In-line Testing

## Slide 4
Photolithography

## Slide 5: Photolithography
    Reticles vs mask
    Light sources
    Photoresist
    Process flow
    Terminologies
    Critical dimension (CD), overlay and inspection

## Slide 6: Comparison be between Photography and Photolithography

## Slide 7: Reticle vs Photomask
Typically used in 1x Contact Aligners
These are used on Steppers or Scanners (5x or 4x)

## Slide 8: Field vs Die
A key concept to introduce at this juncture: Exposure Field vs a Die
Based upon this reticle:
This has an exposure field of 4 x 5 (dies)
Each of the individual squares within is a complete DIE or upon dicing an IC chip.
Singular is called a DIE, multiple DICE.
Each of these are referred to as a DIE
Other features observed on the reticle are unique bar codes that identify the reticle, as well as ‘fudicle’ marks used for the alignment of the reticle to the wafer on the exposure tool.

## Slide 9: Evolution of Exposure Systems
Contact printing
Proximity printing
Projection printing
Step and Repeat / Step and Scan
Layer of Water
The latest innovation is immersion lithography

## Slide 10: Constraints Faced in Photolithography
Key Factors of Consideration
Where k1 = process constant
λ = Wavelength of the illuminating light
NA= Numerical Aperture Of the Lens
DOF Depth of Focus
Where k2 = criteria for acceptable imaging and type of feature
Rayleigh criterion

## Slide 11: Exposure Wavelengths
1980-1990s
g-line – 436nm
h-line – 405nm
1990s-today
i-line – 365nm
DUV -- 248nm (KrF)
193nm (ArF)
Mercury Arc Lamp
Excimer Lasers
One of the key considerations pertains to the intensity of the different light sources used in the exposure, which will directly impact the choice of the photoresist chosen for the application.

## Slide 12: Extreme Ultraviolet (EUV)
KrF and ArF did not contribute to radical changes in the wavelength for the exposure.
In the next leap forward, the industry has adopted EUV lithography, where the wavelength has dropped to 13.5nm.
With the application of RET and OPC techniques, the K1 factor can be reduced, thus providing for geometries of under 9nm can be fabricated in the industry.

## Slide 13: EUV Laser Systems
The system consists of a 40 kW CO2 laser, to create EUV radiation from a 30 µm droplet of tin.
This laser is able to provide a beam intensity of 250W for the exposure of the wafers.
A major shortcoming of this system is the power supply requirements to drive it: 1MW!

## Slide 14: The 2 Families of Photoresist
Exposure
Develop
Etch
Oxide
Substrate
Oxide
UV Light
Substrate
Positive Photoresist
Substrate
Substrate
Resist Strip
UV Light
Substrate
Oxide
Negative Photoresist
Substrate
Oxide
Substrate
Substrate
Positive Resist
Negative Resist
Reticle

## Slide 15: Photolithography Process Flow
Incoming
(film deposition / cleaning step)
Dehydration Bake
Prime (HMDS)
Resist Coat
Soft-Bake
(PAB Bake)
Exposure
Post Exposure Bake (PEB)
Develop
Hard-Bake
Overlay
Inspection
Critical Dimension (CD)
In the modern factories, these steps are performed in an integrated system.

## Slide 16: Common Terminologies in Photolithography
Critical layers vs non-critical layers
Wavelengths
Exposure (E = Intensity x Time)
Reticle Transmission (RT)
ARC, BARC, TARC
Aspect Ratio
CD – critical dimensions
Pitch
Overlay
CAR – chemically amplified resist
PAB (post Apply Bake- soft-bake)
PED (post exposure delay)
Ghost Imaging

## Slide 17: Critical Dimensions Measurements
Measurements made using the scanning electron microscope (SEM).
The tool can be utilized to monitor the line width or the spacing between the photoresist line.
Rudimentary assessments of the profile can be made. For a true understanding of the profiles, a cross-sectional image may be required.

## Slide 18: Comparison between XSEM and OCD
Chart: site 27
| -99.400899999999993 | -84.900899999999993 | -69.150199999999998 | -57.763500000000001 | -55.263500000000001 | -55.263500000000001 | -57.763500000000001 | -55.263500000000001 | 55.263500000000001 | 57.763500000000001 | 55.263500000000001 | 55.263500000000001 | 57.763500000000001 | 69.150199999999998 | 84.900899999999993 | 99.400899999999993
 | 0 | 60.588 | 173.1086 | 384.6859 | 384.6859 | 394.6859 | 394.6859 | 487.0632 | 487.0632 | 394.6859 | 394.6859 | 384.6859 | 384.6859 | 173.1086 | 60.588 | 0
With the introduction of OCD, the next innovation of in-situ metrology is born

## Slide 19: Overlay and Alignment
Overlay ≠ Alignment
A pattern may be said to be well aligned, but the overall overlay of the wafer can still be considered bad leading to wafer being scrapped.
Overlay refers to general pattern placement, whereas alignment refers to specific spots on the wafer (alignment marks or keys). Hence, alignment cannot fully guarantee that the overlay elsewhere upon the wafer meets the desired specifications
However looking at the totality, the resultant overlay is out of the desired specifications.
For the IC’s of today, we are talking about 40+ mask Levels!
Let’s say the alignment specification is ± 0.1 μm, we can say the 2 layers are aligned.